Spectrum Label: Spectrum 1

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 66253

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.61 | 917569 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | -0.20 | -0.18 | -0.27 | Na2O |  |
| Mg K | 4.75 | 4.20 | 7.88 | MgO |  |
| Al K | 37.12 | 29.53 | 70.13 | Al2O3 |  |
| Si K | 4.72 | 3.60 | 10.09 | SiO2 |  |
| P K | 0.07 | 0.05 | 0.15 | P2O5 |  |
| S K | -0.05 | -0.03 | -0.13 | SO3 |  |
| Cl K | -0.09 | -0.06 | 0.00 |  |  |
| K K | -0.23 | -0.13 | -0.28 | K2O |  |
| Ca K | -0.03 | -0.02 | -0.05 | CaO |  |
| Fe L | 9.77 | 3.75 | 12.57 | FeO |  |
| Ni L | 0.00 | 0.00 | 0.00 | NiO |  |
| O | 44.19 | 59.29 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 50

Spectrum Label: Spectrum 2

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 66017

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.63 | 918118 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.28 | 0.25 | 0.38 | Na2O |  |
| Mg K | 4.39 | 3.77 | 7.28 | MgO |  |
| Al K | 40.38 | 31.26 | 76.29 | Al2O3 |  |
| Si K | 5.14 | 3.83 | 11.01 | SiO2 |  |
| P K | -0.40 | -0.27 | -0.92 | P2O5 |  |
| S K | -0.09 | -0.06 | -0.21 | SO3 |  |
| Cl K | 0.04 | 0.03 | 0.00 |  |  |
| K K | -0.19 | -0.10 | -0.23 | K2O |  |
| Ca K | 0.17 | 0.09 | 0.23 | CaO |  |
| Fe L | 5.21 | 1.95 | 6.71 | FeO |  |
| Ni L | -0.46 | -0.16 | -0.58 | NiO |  |
| O | 45.51 | 59.42 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 50

Spectrum Label: Spectrum 3

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 67657

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.55 | 918978 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.04 | 0.04 | 0.05 | Na2O |  |
| Mg K | 5.14 | 4.54 | 8.53 | MgO |  |
| Al K | 36.06 | 28.66 | 68.14 | Al2O3 |  |
| Si K | 4.96 | 3.79 | 10.62 | SiO2 |  |
| P K | 0.22 | 0.15 | 0.51 | P2O5 |  |
| S K | 0.03 | 0.02 | 0.06 | SO3 |  |
| Cl K | -0.01 | 0.00 | 0.00 |  |  |
| K K | 0.03 | 0.02 | 0.04 | K2O |  |
| Ca K | -0.02 | -0.01 | -0.03 | CaO |  |
| Fe L | 9.86 | 3.79 | 12.68 | FeO |  |
| Ni L | -0.47 | -0.17 | -0.59 | NiO |  |
| O | 44.15 | 59.18 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 50

Spectrum Label: Spectrum 4

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 65780

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.58 | 918667 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | -0.20 | -0.18 | -0.26 | Na2O |  |
| Mg K | 3.41 | 2.93 | 5.66 | MgO |  |
| Al K | 41.97 | 32.50 | 79.29 | Al2O3 |  |
| Si K | 4.43 | 3.30 | 9.49 | SiO2 |  |
| P K | 0.10 | 0.07 | 0.24 | P2O5 |  |
| S K | -0.13 | -0.08 | -0.31 | SO3 |  |
| Cl K | 0.20 | 0.12 | 0.00 |  |  |
| K K | 0.20 | 0.11 | 0.24 | K2O |  |
| Ca K | -0.41 | -0.22 | -0.58 | CaO |  |
| Fe L | 4.31 | 1.61 | 5.54 | FeO |  |
| Ni L | 0.39 | 0.14 | 0.50 | NiO |  |
| O | 45.72 | 59.70 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 50

Spectrum Label: Spectrum 5

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 64409

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.52 | 918638 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.15 | 0.13 | 0.20 | Na2O |  |
| Mg K | 1.54 | 1.30 | 2.56 | MgO |  |
| Al K | 47.77 | 36.39 | 90.27 | Al2O3 |  |
| Si K | 2.24 | 1.64 | 4.78 | SiO2 |  |
| P K | -0.08 | -0.05 | -0.18 | P2O5 |  |
| S K | 0.06 | 0.04 | 0.16 | SO3 |  |
| Cl K | -0.25 | -0.14 | 0.00 |  |  |
| K K | 0.47 | 0.25 | 0.56 | K2O |  |
| Ca K | 0.06 | 0.03 | 0.08 | CaO |  |
| Fe L | 1.75 | 0.64 | 2.25 | FeO |  |
| Ni L | -0.34 | -0.12 | -0.44 | NiO |  |
| O | 46.63 | 59.89 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 50

Spectrum Label: Spectrum 6

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 66444

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.66 | 919912 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | -0.14 | -0.13 | -0.19 | Na2O |  |
| Mg K | 4.13 | 3.59 | 6.85 | MgO |  |
| Al K | 40.62 | 31.78 | 76.75 | Al2O3 |  |
| Si K | 3.73 | 2.80 | 7.97 | SiO2 |  |
| P K | -0.11 | -0.08 | -0.26 | P2O5 |  |
| S K | 0.18 | 0.12 | 0.45 | SO3 |  |
| Cl K | -0.05 | -0.03 | 0.00 |  |  |
| K K | -0.15 | -0.08 | -0.18 | K2O |  |
| Ca K | 0.07 | 0.04 | 0.10 | CaO |  |
| Fe L | 6.80 | 2.57 | 8.75 | FeO |  |
| Ni L | -0.15 | -0.05 | -0.19 | NiO |  |
| O | 45.07 | 59.47 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 50

Spectrum Label: Spectrum 7

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 68352

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.72 | 917668 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.14 | 0.14 | 0.19 | Na2O |  |
| Mg K | 4.68 | 4.16 | 7.76 | MgO |  |
| Al K | 36.52 | 29.27 | 69.01 | Al2O3 |  |
| Si K | 4.53 | 3.49 | 9.69 | SiO2 |  |
| P K | -0.01 | -0.01 | -0.03 | P2O5 |  |
| S K | -0.18 | -0.12 | -0.45 | SO3 |  |
| Cl K | -0.15 | -0.09 | 0.00 |  |  |
| K K | 0.09 | 0.05 | 0.11 | K2O |  |
| Ca K | -0.05 | -0.03 | -0.07 | CaO |  |
| Fe L | 11.61 | 4.49 | 14.93 | FeO |  |
| Ni L | -0.78 | -0.29 | -0.99 | NiO |  |
| O | 43.60 | 58.93 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 50

Spectrum Label: Spectrum 8

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 68306

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.66 | 916256 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | -0.07 | -0.06 | -0.09 | Na2O |  |
| Mg K | 4.85 | 4.35 | 8.04 | MgO |  |
| Al K | 35.14 | 28.39 | 66.39 | Al2O3 |  |
| Si K | 4.55 | 3.53 | 9.74 | SiO2 |  |
| P K | 0.04 | 0.03 | 0.10 | P2O5 |  |
| S K | 0.08 | 0.05 | 0.20 | SO3 |  |
| Cl K | -0.03 | -0.02 | 0.00 |  |  |
| K K | 0.04 | 0.02 | 0.04 | K2O |  |
| Ca K | 0.08 | 0.04 | 0.11 | CaO |  |
| Fe L | 11.69 | 4.57 | 15.04 | FeO |  |
| Ni L | 0.36 | 0.13 | 0.46 | NiO |  |
| O | 43.27 | 58.96 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 50

Spectrum Label: Spectrum 9

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 68392

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.59 | 916788 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.07 | 0.06 | 0.09 | Na2O |  |
| Mg K | 4.43 | 3.94 | 7.35 | MgO |  |
| Al K | 37.23 | 29.82 | 70.35 | Al2O3 |  |
| Si K | 4.03 | 3.10 | 8.61 | SiO2 |  |
| P K | 0.04 | 0.03 | 0.09 | P2O5 |  |
| S K | 0.03 | 0.02 | 0.07 | SO3 |  |
| Cl K | 0.01 | 0.01 | 0.00 |  |  |
| K K | -0.03 | -0.02 | -0.04 | K2O |  |
| Ca K | -0.30 | -0.16 | -0.42 | CaO |  |
| Fe L | 11.26 | 4.36 | 14.49 | FeO |  |
| Ni L | -0.47 | -0.17 | -0.60 | NiO |  |
| O | 43.71 | 59.03 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 50