Spectrum Label: Spectrum 1

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 67487

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.50 | 919007 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.20 | 0.19 | 0.28 | Na2O |  |
| Mg K | 3.95 | 3.40 | 6.55 | MgO |  |
| Al K | 41.89 | 32.44 | 79.15 | Al2O3 |  |
| Si K | 3.70 | 2.75 | 7.91 | SiO2 |  |
| P K | -0.08 | -0.05 | -0.18 | P2O5 |  |
| S K | 0.10 | 0.06 | 0.25 | SO3 |  |
| Cl K | -0.08 | -0.04 | 0.00 |  |  |
| K K | -0.31 | -0.16 | -0.37 | K2O |  |
| Ca K | 0.06 | 0.03 | 0.09 | CaO |  |
| Fe L | 5.36 | 2.01 | 6.90 | FeO |  |
| Ni L | -0.39 | -0.14 | -0.49 | NiO |  |
| O | 45.58 | 59.53 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 52

Spectrum Label: Spectrum 2

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 64484

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.56 | 918840 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | -0.08 | -0.07 | -0.11 | Na2O |  |
| Mg K | 1.68 | 1.42 | 2.78 | MgO |  |
| Al K | 47.08 | 35.88 | 88.95 | Al2O3 |  |
| Si K | 2.75 | 2.01 | 5.89 | SiO2 |  |
| P K | -0.13 | -0.08 | -0.29 | P2O5 |  |
| S K | 0.24 | 0.15 | 0.59 | SO3 |  |
| Cl K | 0.19 | 0.11 | 0.00 |  |  |
| K K | -0.14 | -0.07 | -0.17 | K2O |  |
| Ca K | -0.12 | -0.06 | -0.17 | CaO |  |
| Fe L | 1.90 | 0.70 | 2.45 | FeO |  |
| Ni L | -0.08 | -0.03 | -0.11 | NiO |  |
| O | 46.72 | 60.05 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 52

Spectrum Label: Spectrum 3

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 65259

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.47 | 919532 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | -0.07 | -0.06 | -0.09 | Na2O |  |
| Mg K | 1.13 | 0.97 | 1.87 | MgO |  |
| Al K | 42.06 | 32.71 | 79.47 | Al2O3 |  |
| Si K | 0.75 | 0.56 | 1.60 | SiO2 |  |
| P K | -0.06 | -0.04 | -0.15 | P2O5 |  |
| S K | 4.17 | 2.73 | 10.42 | SO3 |  |
| Cl K | 0.08 | 0.04 | 0.00 |  |  |
| K K | 0.16 | 0.09 | 0.20 | K2O |  |
| Ca K | -0.41 | -0.22 | -0.58 | CaO |  |
| Fe L | 5.31 | 2.00 | 6.83 | FeO |  |
| Ni L | 0.29 | 0.10 | 0.37 | NiO |  |
| O | 46.61 | 61.12 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 52

Spectrum Label: Spectrum 4

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 68409

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.54 | 916901 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | -0.06 | -0.06 | -0.08 | Na2O |  |
| Mg K | 5.13 | 4.46 | 8.50 | MgO |  |
| Al K | 38.34 | 30.02 | 72.44 | Al2O3 |  |
| Si K | 4.63 | 3.48 | 9.91 | SiO2 |  |
| P K | 0.28 | 0.19 | 0.65 | P2O5 |  |
| S K | -0.08 | -0.05 | -0.20 | SO3 |  |
| Cl K | 0.12 | 0.07 | 0.00 |  |  |
| K K | 0.07 | 0.04 | 0.09 | K2O |  |
| Ca K | 0.00 | 0.00 | 0.01 | CaO |  |
| Fe L | 7.35 | 2.78 | 9.46 | FeO |  |
| Ni L | -0.69 | -0.25 | -0.88 | NiO |  |
| O | 44.90 | 59.31 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 52

Spectrum Label: Spectrum 5

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 68185

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.55 | 917265 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | -0.12 | -0.12 | -0.17 | Na2O |  |
| Mg K | 3.51 | 3.12 | 5.83 | MgO |  |
| Al K | 37.67 | 30.14 | 71.18 | Al2O3 |  |
| Si K | 3.47 | 2.67 | 7.42 | SiO2 |  |
| P K | -0.07 | -0.05 | -0.16 | P2O5 |  |
| S K | 0.98 | 0.66 | 2.45 | SO3 |  |
| Cl K | 0.02 | 0.01 | 0.00 |  |  |
| K K | 0.05 | 0.03 | 0.06 | K2O |  |
| Ca K | 0.20 | 0.11 | 0.28 | CaO |  |
| Fe L | 10.01 | 3.87 | 12.88 | FeO |  |
| Ni L | 0.17 | 0.06 | 0.22 | NiO |  |
| O | 44.11 | 59.51 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 52

Spectrum Label: Spectrum 7

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 69260

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.49 | 917344 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | -0.01 | -0.01 | -0.01 | Na2O |  |
| Mg K | 4.44 | 3.96 | 7.37 | MgO |  |
| Al K | 37.37 | 29.98 | 70.60 | Al2O3 |  |
| Si K | 3.51 | 2.71 | 7.51 | SiO2 |  |
| P K | 0.14 | 0.10 | 0.33 | P2O5 |  |
| S K | 0.02 | 0.01 | 0.05 | SO3 |  |
| Cl K | -0.16 | -0.10 | 0.00 |  |  |
| K K | 0.15 | 0.09 | 0.19 | K2O |  |
| Ca K | 0.27 | 0.15 | 0.38 | CaO |  |
| Fe L | 10.86 | 4.21 | 13.97 | FeO |  |
| Ni L | -0.17 | -0.06 | -0.22 | NiO |  |
| O | 43.57 | 58.97 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 52

Spectrum Label: Spectrum 8

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 68888

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.54 | 916629 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.06 | 0.05 | 0.08 | Na2O |  |
| Mg K | 4.76 | 4.21 | 7.89 | MgO |  |
| Al K | 37.38 | 29.80 | 70.62 | Al2O3 |  |
| Si K | 4.21 | 3.22 | 9.00 | SiO2 |  |
| P K | -0.14 | -0.10 | -0.33 | P2O5 |  |
| S K | 0.06 | 0.04 | 0.14 | SO3 |  |
| Cl K | -0.21 | -0.13 | 0.00 |  |  |
| K K | 0.10 | 0.06 | 0.12 | K2O |  |
| Ca K | -0.15 | -0.08 | -0.21 | CaO |  |
| Fe L | 10.14 | 3.91 | 13.05 | FeO |  |
| Ni L | -0.12 | -0.04 | -0.15 | NiO |  |
| O | 43.92 | 59.06 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 52

Spectrum Label: Spectrum 9

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 65297

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.48 | 919025 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.16 | 0.14 | 0.21 | Na2O |  |
| Mg K | 2.54 | 2.18 | 4.20 | MgO |  |
| Al K | 43.84 | 33.97 | 82.82 | Al2O3 |  |
| Si K | 3.05 | 2.27 | 6.53 | SiO2 |  |
| P K | -0.19 | -0.13 | -0.43 | P2O5 |  |
| S K | 0.15 | 0.10 | 0.37 | SO3 |  |
| Cl K | -0.08 | -0.04 | 0.00 |  |  |
| K K | 0.50 | 0.27 | 0.60 | K2O |  |
| Ca K | 0.03 | 0.01 | 0.04 | CaO |  |
| Fe L | 4.85 | 1.82 | 6.24 | FeO |  |
| Ni L | -0.41 | -0.15 | -0.52 | NiO |  |
| O | 45.56 | 59.55 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 52