

Spectrum Label: Spectrum 1

Livetime 90.0 s

Acquisition geometry ( degrees ):

 Tilt = 0.0

 Azimuth = 0.0

 Elevation = 30.0

 Accelerating voltage = 10.00 kV

 Total spectrum counts = 60835

|  |  |  |  |
| --- | --- | --- | --- |
| Sample data : | Energy (eV) | Resn. (eV) | Area |
| Strobe : | 3.8 | 40.40 | 950373 |
|  |  |  |  |
| Optimization data : Cobalt K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 41.16 | 1008028 |
| Optimization element : | 6916.2 | 136.04 | 88085 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Mg MgO 1-Jun-1999 12:00 AM

Al Al2O3 1-Jun-1999 12:00 AM

Si SiO2 1-Jun-1999 12:00 AM

Ca Wollastonite 1-Jun-1999 12:00 AM

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Element | Weight% | Atomic% | Compd% | Formula |  |
|   |   |   |   |   |  |
| Mg K | 2.18 | 1.85 | 3.61 | MgO |  |
| Al K | 41.34 | 31.55 | 78.11 | Al2O3 |  |
| Si K | 6.40 | 4.69 | 13.68 | SiO2 |  |
| Ca K | 3.28 | 1.69 | 4.59 | CaO |  |
| O | 46.80 | 60.23 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project: Project 1

Owner: Operator

Site: Site of Interest 63